## Slide 1
Status of SEY-R benchmarking with 25 ns data
O. Domínguez, G. Rumolo
Thanks to
M. Taborelli, C. Yin Vallgren, G. Lanza
28 November 2011 - e- cloud meeting

## Slide 2
Outline
28 November 2011 - e- cloud meeting
Data analysis from MD 25 October 2011
Stainless Steel emax evolution
  In the lab (e- gun)
  In the beam pipe
25 ns thresholds and estimation of scrubbing time
Conclusions

## Slide 3
Outline
28 November 2011 - e- cloud meeting
Data analysis from MD 25 October 2011
Stainless Steel emax evolution
  In the lab (e- gun)
  In the beam pipe
25 ns thresholds and estimation of scrubbing time
Conclusions

## Slide 4
Batch spacing dependence experiment: 9h00 – 9h30
Filling scheme:
The pressure decrease after every injection is not any more observed
Some more time would be good to achieve steady state pressure after every two injections, but the results look quite promising
It is a (relatively) fast measurement
4 ms
3 ms
2 ms
1 ms
16.5 ms
16.5 ms
16.5 ms
72b
MD 25/10/2011
28 November 2011 - e- cloud meeting
As a reminder….

## Slide 5
4 ms
3 ms
2 ms
1 ms
MD 25/10/2011
28 November 2011 - e- cloud meeting
As a reminder….

## Slide 6
28 November 2011 - e- cloud meeting
MD 25/10/2011
Gauge VGPB.2.5L3.B
emax = 230 eV

## Slide 7
28 November 2011 - e- cloud meeting
MD 25/10/2011
Gauge VGPB.2.5L3.B
emax = 260 eV

## Slide 8
28 November 2011 - e- cloud meeting
MD 25/10/2011
Gauge VGPB.2.5L3.B
emax = 200 eV

## Slide 9
28 November 2011 - e- cloud meeting
MD 25/10/2011
Unfortunately no agreement is found for the gauge VGI.141.6L4.B
This can be caused by the indeed worse fit surfaces (the lower the pressure, the worse is generally the fit)
The good point is that the lines are not found when exploring higher dmax values, i.e. This should be the area where one should find the right value
Actually this should be 0.025
Different values of emax just move the lines to the right or to the left

## Slide 10
Outline
28 November 2011 - e- cloud meeting
Data analysis from MD 25 October 2011
Stainless Steel emax evolution
  In the lab (e- gun)
  In the beam pipe
25 ns thresholds and estimation of scrubbing time
Conclusions

## Slide 11
28 November 2011 - e- cloud meeting
emax evolution
emax apparently evolves in a different way depending on the experiment
emax doesn’t change much
This slight change is an increase
StSt as received: emax ≈ 282 eV (normally I have used 230 eV for all my simulations)
Cu shows a similar behavior (with emax ≈ 332 eV as received)
In the lab (e- gun)
C. Yin Vallgren

## Slide 12
28 November 2011 - e- cloud meeting
emax evolution
emax apparently evolves in a different way depending on the experiment
emax change is more significant
This change shows a reduction (from ~282 eV to ~200 eV)
There aren’t many experimental data for StSt
Cu shows a similar behavior (there are more experimental data with beam)
In the beam pipe (scrubbing)
C. Yin Vallgren

## Slide 13
Outline
28 November 2011 - e- cloud meeting
Data analysis from MD 25 October 2011
Stainless Steel emax evolution
  In the lab (e- gun)
  In the beam pipe
25 ns thresholds and estimation of scrubbing time
Conclusions

## Slide 14
28 November 2011 - e- cloud meeting
25 ns thresholds
emax (eV) | Threshold (R=0.2) | Threshold (R=0.3) | Threshold (R=0.4)
180 | 1,2 | 1,2 | 1,15/1,2
230 | 1,25 | 1,25 | 1,2/1,25
280 | 1,3 | 1,3 | 1,25/1,3
The thresholds are the same for both gauges explored

## Slide 15
28 November 2011 - e- cloud meeting
Estimation of scrubbing time
(Rough) Estimation of the scrubbing time
I consider results from the last MD (25 October): R=[0.2, 0.4] and dmax=[1.3, 1.4]
I consider the configuration with bunches separated by 1 ms
I calculate the # of e- impinging the wall after the passage of 1 and 2 batches, take the difference and multiply by 2 (if the machine is filled in, that will be more realistic):
I integrate this amount by the corresponding time (~ 5 ms) and multiply by e
I consider an estimate dose from C. Yin Vallgren plots and divide it by the previous number
x2

## Slide 16
28 November 2011 - e- cloud meeting
Estimation of scrubbing time
Is there a scrubbing limit for StSt at dmax≈ 1.25 ??
Lab (e- gun)
SPS (scrubbing)
C. Yin Vallgren
dmax | 1.3 | 1.3 | 1.3 | 1.35 | 1.35 | 1.35 | 1.4 | 1.4 | 1.4
R | 0.2 | 0.3 | 0.4 | 0.2 | 0.3 | 0.4 | 0.2 | 0.3 | 0.4
t1 (~days) | 38 | 23 | 15 | 11 | 8 | 7 | 6 | 5 | 5
t2 (~days) | 230 | 70 | 30 | 11 | 9 | 8 | 6 | 5 | 5
emax = 230 eV ; Dose = 1.67 ∙ 10-2 C/mm2 – Threshold dmax ≈ 1.25
t1 = Time necessary to scrubb until threshold for VGPB.2.5L3.B
t2 = Time necessary to scrubb until threshold for VGI.141.6L4.B (assuming same initial condtions as for VGPB.2.5L3.B)

## Slide 17
28 November 2011 - e- cloud meeting
Estimation of scrubbing time
Is there a scrubbing limit for StSt at dmax≈ 1.25 ??
Lab (e- gun)
SPS (scrubbing)
C. Yin Vallgren
dmax | 1.3 | 1.3 | 1.3 | 1.35 | 1.35 | 1.35 | 1.4 | 1.4 | 1.4
R | 0.2 | 0.3 | 0.4 | 0.2 | 0.3 | 0.4 | 0.2 | 0.3 | 0.4
t1 (~days) | 190 | 115 | 50 | 14 | 8 | 5 | 5 | 4 | 3
t2 (~days) | 1000 | 600 | 300 | 31 | 15 | 8 | 5 | 4 | 3
emax = 260 eV ; Dose = 7.5 ∙ 10-3 C/mm2 – Threshold dmax ≈ 1.3
t1 = Time necessary to scrubb until threshold for VGPB.2.5L3.B
t2 = Time necessary to scrubb until threshold for VGI.141.6L4.B (assuming same initial condtions as for VGPB.2.5L3.B)

## Slide 18
28 November 2011 - e- cloud meeting
Estimation of scrubbing time
Lab (e- gun)
SPS (scrubbing)
C. Yin Vallgren
Can we conclude that the scrubbing takes longer (~twice?) in the machine??

## Slide 19
Outline
28 November 2011 - e- cloud meeting
Data analysis from MD 25 October 2011
Stainless Steel emax evolution
  In the lab (e- gun)
  In the beam pipe
25 ns thresholds and estimation of scrubbing time
Conclusions

## Slide 20
28 November 2011 - e- cloud meeting
Conclusions
New scrubbing status results have been shown: R=[0.2, 0.4] and dmax=[1.3, 1.4]
No agreement was found for gauge VGI.141.6L4.B, possibly due to worse fitting functions This point must be further studied
Evolution of emax has been shown in different situations (lab and beam pipe)
It could be interesting to revise all previous benchmarking results for different emax values (e.g. 280 eV)
Thresholds for 25 ns has been pointed out for different emax values
A rough estimation for the time necessary to scrubb until threshold values has been given

## Slide 21
THANK YOU FOR YOUR ATTENTION